CME 785

SCANNING ELECTRON MICROSCOPY

Fall Semester 2010

Monday, August 30

Lecture:		Introduction

Demonstration:	 	Operation of the SEM

Readings:		SEM Student Handbook, pp. 1-47

Wednesday, September 1

Lecture:		Operation of the Microscope

Filament saturation

Module-by-module description of the SEM

Cautions

Demonstration:	Microscope operation

Readings:	Handout – Operation Manual

Lab:	Individual Instruction

## Monday, September 6	Labor day – No Class

Lab: Individual Instruction continued

Wednesday, September 8

Lecture:		Vacuum Systems:  Theory and Applications

What is High Vacuum?

The Mechanical Pump

The Oil Diffusion Pump

Secondary Electron Signal

Spot Size

Resolution

Signal

Monday, September 13

Lecture:		Specimen Preparation I - Coating Specimens

The generation of secondary electrons and the need for specimen coating

Sputter coating

High vacuum evaporation

Osmium-thiocarbohydrazide-osmium impregnation

Random potentials

Uncoated specimens

Digital Image Acquisition, Annotation,Transfer and Save

Demonstration:		Operation of the sputter coater

Readings:		Operation Manual for Denton Sputter Coater

SEM Student Handbook, pp. 145-168

Laboratory	Sputter coat a specimen (paper or a dry specimen of your choice) and produce a micrograph of it

Assignment:		Save an Image to Personal folder on Data G

( Due 9/15)

Wednesday, September 15

Lecture:		Specimen Preparation II - Specimen Drying

Fixation

Critical Point Drying

Freeze Drying

Chemical Dehydration

Artifacts

Demonstration:		Use of the Critical Point Drying Apparatus

Operation of the SEM

Readings:		SEM Student Handbook, pgs. 115-145

Laboratory		Prepare a fungal sample utilizing the critical point drying apparatus and  TMS		Assignment:		produce 1 micrograph utilizing each technique   (DUE:  9/22)

Monday, September 20

Lecture:		Accelerating Voltage and Filament Saturation

Edge Effect

Laboratory		3 micrographs demonstrating the choice of accelerating voltage (insect

Assignment:		or fungi, minimum magnification 1000x)  (DUE: 9/22)

Reading

Assignment:		SEM Student Handbook, pp. 47-65

Wednesday, September 22

Optimizing Depth of Field

Discussion of  the factors which affect depth of field

Apertures – Use and Alignment

Laboratory		4 micrographs demonstrating effect of working distance on depth of

Assignment:		field (gold grid tilted 60(, 1200x)    (DUE 9/27)

Buy  Epson Photo Quality Paper- Glossy  ( for 9/29 lab)

Monday , September 27

Lecture:		Resolution

The concept of resolution

Factors which limit resolution

Astigmatism—Its cause and correction

Laboratory		4 micrographs demonstrating effect of spot size, working distance,

Assignment:		and astigmatism on resolution and contrast (gold grid at 20,000x,30,000x)

(DUE:  10/4)

#### Wednesday, September 29

Digital Darkroom I

Lecture:		Pixelated Images and Histograms

Contrast Enhancement

Photoshop I

Printing Digital Images

Adding Text

Laboratory

Assignment:		Print Two SEM Images (Due 10/4)

Monday, October 4

Cryofracture

Laboratory

Assignment:		One micrograph utilizing cryofracture (Due 10/11)

Wednesday, October 6

Digital Darkroom II

Look-up Tables

Transforming Black and white images into color

Discussion of  Final Projects

Laboratory

Assignment:		Print a micrograph to which color has been added (Due 10/11)

Monday, October 11

Use of Apertures

Review for Exam

Wednesday, October 13

EXAM I

Monday, October 18

Stereo Microscopy

Laboratory

Assignment:		Take a Stereo Pair (Due 10/20)

Wednesday, October 20

Low Accelerating Voltage

Digital Darkroom III

Laboratory

Assignment:		Print a Red-Green Stereo Pair (Due 10/25)

Monday, October 25

Lecture:		Primary (Backscattered electron) Mode of Operation

Generation of the primary image

Biological applications

The use of heavy metal stains and markers

Demonstration:	Operation of the backscatter detector

Readings:		Primary mode of operation hand-out

Laboratory		1 micrograph utilizing the primary mode of operation (crystals

Assignment:		in wood)   (DUE:  10/27)

Wednesday, October 27

Backscatter (cont’d)

Digital Darkroom IV

Image Processing

Noise reduction, sharpen, unsharp mask

##### Laboratory

##### Assignment:		1 micrograph utilizing BSE for Atomic Number Contrast

##### 1  micrograph demonstrating sharpen or unsharp masking	( Due 11/1 )

##### Monday, November 1

Lecture:		Energy-Dispersive X-ray Analysis I

The generation of x-rays in the SEM

X-ray detection

Interpretation of spectra and artifacts

Demonstration:		Operation of EDXA System

Readings:		SEM Student Handbook, pp. 69-111

Operation of  EDXA Handout

Laboratory

Assignment:		An x-ray spectrum of a known

(DUE:  11/3)

Wednesday, November 3

Discussion of Final Projects II

EDXA Unknowns

Monday, November 8

Lecture:		EDXA II

Elemental Mapping

TRIX

Line Scan

Spot Analysis

Quantitation

Demonstration:	TRIX

Elemental Mapping

Line Scan

Laboratory		An Elemental Map

Assignment:			(DUE:  11/10)

Wednesday, November 10

Transmission Electron Microscopy

Monday, November 15

Review

Wednesday, November 17

EXAM II

Monday, November 22		 Light Microscopy

Wednesday, November 24

Thanksgiving Recess

Monday, November 29

Final Project Progress Assessment

Wednesday,  December 1

Final Project Progress Assessment

Monday, December 6

Low Vacuum Operation

Wednesday, December 8

No Class

Friday, December 10

Projects Due at 4:00 P.M.

Students submit projects and micrographs.  Students return

keys, cleaned SEM stubs, and specimen boxes.

Grades will not be submitted to Registrar until all materials have

been accounted for.

REQUIREMENTS FOR THE ERE 785FINAL PROJECT

Part I  -  A portfolio of micrographs demonstrating the following techniques

1. Critical Point Drying

2. Depth of Field

3. Backscatter*

4. Energy Dispersive X-ray Analysis*

5. High Magnification (>50,000 )

6. Stereo Pair

7. Cryofracture

8. Aesthetic (Optional)

* - must be accompanied be a secondary image of the same

Part II  –  Publication Micrograpghs -  The micrograpghs should be presented as if they were to be submitted for publication in a national peer reviewed journal. This includes Figure Legends with final magnifications.

- A series of micrographs relating to a biological specimen

- A series of micrographs relating to a non-biological specimen

A minimum of 8 micrographs relating to each subject

No more than 3 micrographs from Part I  may be used in Part II

TEXT

Scanning Electron Microscopy – A Students Handbook, Postek et al.,Ladd Research Inc.

STUDENT LEARNING OUTCOMES:

After completing this course the student should be able to:

- Understand the theory and use of the scanning electron microscope (SEM) as a scientific tool

- To have knowledge of the wide range of scanning electron microscope techniques currently available (secondary, backscatter, x-ray, field emission, cryo)

- To be able to determine the type of specimen preparation techniques necessary for biologic and non-biologic specimens

- To be able to interpret artifacts and specimen structures based on the type of image and specimen preparation

- To be able to prepare specimens for examination with the SEM using the techniques of fixation, drying, sputter coating, carbon coating, rotary shadowing, HVEM.

- To be able to capture and prepare digital images of a variety of samples

- To have awareness of other advanced microscopy techniques such as light microscopy, transmission electron microscopy, confocal and others, and the appropriate technique for the sample and research goal.

- Operate a scanning electron microscope for an employer.

MAJOR CONCEPTS OR METHODOLOGIES:

This course will cover the theory and operation of scanning electron microscopes.  Concepts include resolution versus contrast, signal generation, accelerating voltage, spot size, apertures.  Other concepts to be covered are the reasons for choosing the appropriate specimen preparation technique for both biological and non-biological samples, artifacts due to specimen preparation, and artifacts introduced during image generation, as well as digital image acquisition and introductory image processing.